| CHEMOTEX Děčín a. s. Děčín XXXII – Boletice nad Labem 63 407 11 Děčín \u268 Ceská republika | Tel: +420-412-547 461 Fax: +420-412-547 200 E-mail: chemotex@chemotex.cz www.chemotex.cz |
| --- | --- |
| EBOL DEKARB |
| TECHNICAL DATA SHEET TL 364/2004 |
| Date of issue: 1.12.2004 | Revision date: 1.7.2014 |

Product characteristics:

Mixture of surface active substances and organic agents.

Application

Industrial agent with increased cleaning ability for surfaces contaminated with hard black carbon coating. The agent is also used for removing grease and old paints from metal surfaces.

It is suitable for cleaning the materials – magnesium alloy, aluminium and its alloys, copper and its alloys, steel, etc.

It can be suitable used for the removal of the defined layers and contaminations, e.g. from surfaces of the parts in aviation and automotive motors.

Properties of the product

EBOL DEKARB is yellowish liquid. It efficiently replaces the classic cleaning agents on chlorinated hydrocarbons base, petrol, or oil degreasing agents, and it works in locations these agents fail. The agent does not contain phenol, phosphates, and chloride treated hydrocarbons.

The agent does not have corrosive effects on steel, electron (magnesium alloy), aluminium, and copper and its alloys.

EBOL DEKARB must comply with these quality signs:

| Quality mark | Value | Determination methodology |
| --- | --- | --- |
| pH sample | 12.5 to 13.5 | PN-ZM 364/2004 |
| Density at 20 °C in kg.m-3 | min 1000 | ČSN 65 0342 |

Product processing

Concentrated agent is used for cleaning and removal of paints. Water must not be added in the product! Water has adverse effects due to possible corrosion of cleaned products.

The most suitable application is the submersion of cleaned product or material in concentrated agent EBOL DEKARB. It is recommended to have reserve  EBOL DEKARB for bath filling in the amount approximately 25 % of total bath volume.

The agent can be used at common and increased temperature. .  The higher temperature, the faster effect. The agent can be heated to 80 °C. We do not recommend higher temperature due to safety reasons. The ignition point of the agent is approx 90 °C.

| Temperature (°C) | Exposure time (hours) |
| --- | --- |
| 25 | 24 to 72 |
| 80 | 2 to 8 |

The defined exposure period can be reduced and extended. It depends on the level of carbonising of the surface and hardness, eventually the compactness of carbon coating.  The rinsing can be performed with high pressure steam cleaning.

The application can be performed e.g. in steel (stainless) bath, it is impossible to use plastic vessels.

Cleaned parts must not contain rubber or plastic parts.

Packaging, storage

EBOL DEKARB is supplied in metal barrels of 200 litre volumes or in other pre-agreed containers.

It is stored in closed containers in the locations protected from direct weather conditions. Recommended storage temperature is +5 to +25 °C.

Transport

EBOL DEKARB is transported in covered transport vehicles in compliance with regulations ADR/RID.

Warranty period and service life

If the product is transported and stored according to the above-mentioned conditions, the warranty is 6 months from the date of warehouse delivery.

The service life is 36 months from the date of delivering from the warehouse. During storage, observe the recommended storage conditions.

Note

The data on the product properties and its processing were received by laboratory measuring and application tests. This technical data sheet can be used for reference purposes, the product processing must be adapted to the specific conditions.