| CHEMOTEX Děčín a. s. Děčín XXXII – Boletice nad Labem 63 407 11 Děčín \u268 Ceská republika | Tel: +420-412-547 461 Fax: +420-412-547 200 E-mail: chemotex@chemotex.cz www.chemotex.cz |
| --- | --- |
| KORYNT CH 50/50 |
| TECHNICAL DATA SHEET TL 773/2016 |
| Date of issue: 20.10.2016 | Revision date: - |

Product characteristics:

KORYNT CH 50/50 is highly effective mixture of organic solvents.

Application

KORYNT CH 50/50 is designed specially for degreasing the steel wires designed for cords of tyres. It can also be used for degreasing and cleaning the metal surfaces, machine parts, and various parts of railway wagons and other machine devices from vaseline and fat on metal soap base.

### Properties of the product

KORYNT CH 50/50 is low viscosity liquid, not miscible with water. It is highly flammable liquid. It is necessary to observe all safety measures for work with highly flammable substances!!

KORYNT CH 50/50 must comply with these quality signs:

| Quality mark | Value | Determination methodology |
| --- | --- | --- |
| Density 20 °C in kg.m-3 | 755 to 775 | PN-ZM 773/2016 |
| Appearance | Clear, colourless to light yellow liquid | Visual |

Organic solvent content

| characteristics | unit | value |
| --- | --- | --- |
| Product density | g.cm-3 | 0,770 |
| Content of organic solvents expressed as weight fraction | kg/kg of product | 1,0 |
| Content of total organic carbon | kg/kg of product | 0,88 |
| Content of non-volatile substances expressed in % volume | % Volume | 0,0 |

#### Product processing

KORYNT CH 50/50 is designed specially for cleaning and degreasing metal objects and machine parts.

Packaging, storage

KORYNT CH 50/50 is available in metal drums of 200 litre volumes or in other pre-agreed containers.  It is stored in closed containers in the locations protected from direct weather conditions. Recommended storage temperature is +5 to +25 °C. Storage at temperatures below 0 °C has no negative effect on the application characteristics of the product.

Transport

KORYNT CH 50/50 is highly flammable mixture, transported in covered transport vehicles in compliance with regulations ADR/RID.

Guarantee period

If the product is transported and stored according to the above-mentioned conditions, the warranty is 24 months from the date of warehouse delivery.

Note

The data on the product properties and its processing were received by laboratory measuring and application tests. This technical data sheet can be used for reference purposes, the product processing must be adapted to the specific conditions.